## Slide 1
GaInSb-TQW auf GaSb
Phase diagram from the Nextnano simulations for InAs-Ga68In32Sb-InAs on GaSb substrate with different crystal directions (001 & 111)
001
111

## Slide 2
Differences: (example 5 nm InAs – 4 nm GaInSb – 5 nm InAs)
The QSHI phase starts at smaller InAs values for the 111 Substrate direction  Band inversion between E1 & H1 takes place earlier  H1 state is shifted to higher values
001
111
Band & state shifts

## Slide 3
Band & state shifts
Differences: (example 5 nm InAs – 4 nm GaInSb – 5 nm InAs)
The QSHI phase starts at smaller InAs values for the 111 Substrate direction  Band inversion between E1 & H1 takes place earlier  H1+H2 state is shifted to higher values & E1+E2 is shifted to lower values
 REASON: „strain“ behavior caused by the difference in crystal direction which resulsts in different lattice constant

## Slide 4
Maximum gap position
Differences:
The InAs thickness where the TQWs show the maximum gap is shifted to lower InAs thicknesses

## Slide 5
Maximum gap values
Differences:
The Maximum Gap value is higher for the 111 substrate crystall direction

## Slide 6
Phase diagram shift
Differences:
The HOTI phase is shifted to smaller GaInSb thicknesses and resulting from the shifted bands and states, the HOTI phase also evolves at smaller InAs thicknesses
001
111

## Slide 7
Gap evolution
Differences:
The gap evolution is shifted to smaller InAs values for 111 compared to 001
001
111

## Slide 8
Gap evolution
Differences: (example X nm InAs – 5 nm GaInSb – X nm InAs)
The gap evolution is shifted to smaller InAs values for 111 compared to 001
001
111

## Slide 9
Difference in SM phase
Differences: (example X nm InAs – 5 nm GaInSb – X nm InAs)
As the TQW with 111 substrate is already near the region where the HOTI phase opens up, the „gap values“ for the SM remain almost constant (instead of decreasing)
 but the HOTI phase does not open yet  TQW remains SM